## Slide 1: ALE3D Simulations of Laser Heating Steel
Zhigang Wu
May 08, 2019

## Slide 2: ALE3D Default Units
Length: 1 cm = 0.01 m
Volume: 1 cc = 1 cm3 = 10-6 m3
Mass: 1 g = 10-3 kg
Time: 1 μs = 10-6 s
Pressure: 1 Mbar = 1011 Pa
Energy: 1 Mbar∙cc = 105 J
Power: 1 Mbar∙cc/μs = 1011 W
Temperature: 1 K
https://wci.llnl.gov/simulation/computer-codes/ale3d

## Slide 3: Notes
Turning on axis-symmetry leads to failure—fixed by changing the integrator.
All the 2D simulations were redone with axis-symmetry (x-axis).
Technical points in ALE3D simulations:
  The x-axis is always the rotation axis in 2D calculation when the axis-symmetry is turned on.
  In present calculations because the energy density is very high near the axis, a mode is erroneously excited using the default integrator.
  No physics of laser-plasma interaction is implemented in ALE3D, so the absorption table is constructed using a simple linear rule: extinction parameter is proportional to density. Using available experimental data, or set the parameter based on zone size; e.g., for millimeter zoning, set absorb = 10 cm-1.

## Slide 4: ALE3D Parallel Calculation
Partition: multiple of # of cores
Decomp block
-p in command line
4 times faster in parallel

## Slide 5: Cross-Section of Laser Heating Steel Substrate (Bulk)
J. Heat Transfer 131, 072101 (2009)

## Slide 6: Previous ALE3D Simulations
J. Mater. Proc. Tech. 214, 2627 (2014)

## Slide 7: Property Parameters For Steel (Stainless, 316L)
Melting point: 1700 K
Thermal conductivity:
  20 W/m∙K = 20×10-13 Mbar∙cc/cm∙μs∙K
Thermal capacity:
  0.5 J/g∙K = 0.5×10-5 Mbar∙cc/g∙K
Optical properties:
  Absorptivity: 44% (reflectivity: 56%)
  Extinction coefficient (bulk): 7.53×105 cm-1
  Extinction coefficient (d = 57 μm, powder): 500 cm-1
J. Appl. Phys. 98, 013533 (2005)

## Slide 8: Parameters For Laser
Shape and Size
  Circular
  Gaussian
kG: Gaussian parameter
kG = 0.6 (default), FWHM = 0.353w (w: width)
at the edge (r = w/2), p = 0.004 p0

## Slide 9: Parameters For Laser
Shape and Size
  Circular
  Gaussian
  FWHM: 50 μm
  w: 141.6 μm
  FWHM: 60 μm
  w: 169.9 μm
  Power (P):
  22.5 W & 45 W
P = 22.5 W, FWHM = 50 μm, p0 = 7.94×105 W/cm2
P = 45.0 W, FWHM = 60 μm, p0 = 1.10×106 W/cm2

## Slide 10: Present ALE3D Simulations
Power: 22.5 W; FWHM: 50 𝜇m; p0 = 7.94×105 W/cm2; scanning speed v = 0
Absorptivity: 0.44; Extinction coefficient 𝛽: 7.53×105 cm-1 (bulk)
t = 30 𝜇s
Start to melt: Reaching 1700 K
10-3 cm = 10 𝜇m

## Slide 11: Present ALE3D Simulations
Power: 22.5 W; FWHM: 50 𝜇m; p0 = 7.94×105 W/cm2; scanning speed v = 0
Absorptivity: 0.44; Extinction coefficient 𝛽: 7.53×105 cm-1 (bulk)
t = 170 𝜇s
melt width: 36 𝜇m
melt depth: 4.5 𝜇m
width:depth = 8:1

## Slide 12: Present ALE3D Simulations
Power: 22.5 W; FWHM: 50 𝜇m; p0 = 7.94×105 W/cm2; scanning speed v = 0
Absorptivity: 0.44; Extinction coefficient 𝛽: 7.53×105 cm-1 (bulk)
t = 670 𝜇s
melt width: 79 𝜇m
melt depth: 23 𝜇m
width:depth = 3.4:1

## Slide 13: Present ALE3D Simulations
Power: 22.5 W; FWHM: 50 𝜇m; p0 = 7.94×105 W/cm2; scanning speed v = 0
Absorptivity: 0.44; Extinction coefficient 𝛽: 7.53×105 cm-1 (bulk)

## Slide 14: Present ALE3D Simulations
Power: 22.5 W; FWHM: 50 𝜇m; p0 = 7.94×105 W/cm2; v = 0
Absorptivity: 0.44; Extinction coefficient 𝛽: 500 cm-1 (powder, d = 57 𝜇m)
t = 470 𝜇s
Start to melt
10-3 cm = 10 𝜇m

## Slide 15: Present ALE3D Simulations
Power: 22.5 W; FWHM: 50 𝜇m; p0 = 7.94×105 W/cm2; v = 0
Absorptivity: 0.44; Extinction coefficient 𝛽: 500 cm-1 (powder, d = 57 𝜇m)
t = 670 𝜇s
melt width: 50 𝜇m
melt depth: 25 𝜇m
width:depth = 2:1

## Slide 16: Present ALE3D Simulations
Power: 22.5 W; FWHM: 50 𝜇m; p0 = 7.94×105 W/cm2; v = 0
Absorptivity: 0.44; Extinction coefficient 𝛽: 500 cm-1 (powder, d = 57 𝜇m)
t = 800 𝜇s
melt width: 72 𝜇m
melt depth: 42 𝜇m
width:depth = 1.7:1

## Slide 17: Present ALE3D Simulations
Power: 22.5 W; FWHM: 50 𝜇m; p0 = 7.94×105 W/cm2; v = 0
Absorptivity: 0.44; Extinction coefficient 𝛽 are different
500 cm-1 (powder, d = 57 𝜇m)
7.53×105 cm-1 (bulk)
t = 780 𝜇s
width/depth = 3/1
t = 670 𝜇s
width/depth = 2/1

## Slide 18: Present ALE3D Simulations
Power: 22.5 W; FWHM: 50 𝜇m; p0 = 7.94×105 W/cm2; v = 0
Absorptivity: 0.44; Extinction coefficient 𝛽 are different
Width-to-depth ratio
Melt width and depth

## Slide 19: Present ALE3D Simulations
v = 0; absorptivity: 0.44; 𝛽: 7.53×105 cm-1
P = 22.5 W, FWHM = 50 𝜇m
p0 = 7.94×105 W/cm2
t = 200 𝜇s, width/depth = 4/1
P = 45 W, FWHM = 60 𝜇m
p0 = 11.03×105 W/cm2
t = 780 𝜇s
width/depth = 3/1

## Slide 20: Present ALE3D Simulations
Power: 22.5 W; FWHM: 50 𝜇m; p0 = 7.94×105 W/cm2; v = 0
Extinction coefficient 𝛽: 7.53×105 cm-1 (bulk)
Absorptivity: 0.30
Absorptivity: 0.44
t = 150 𝜇s, starts to melt
t = 800 𝜇s, width/depth = 5/1
t = 780 𝜇s
width/depth = 3/1

## Slide 21: Laser Scanning
q0 is the maximum incident energy per unit area (J/cm2)
For on-spot laser (v = 0)
P = 22.5 W, FWHM = 50 𝜇m, v = 15 cm/s, q0 = 282 J/cm2
P = 45.0 W, FWHM = 60 𝜇m, v = 30 cm/s, q0 = 235 J/cm2
Assuming laser is circular:

## Slide 22: Present ALE3D Simulations
3D simulations for scanning laser
Scanning speed v = 15 cm/s
P = 22.5 W; FWHM = 50 𝜇m
q0 = 282 J/cm2
𝜏 = FWHM/v = 333 𝜇s
Absorptivity: 0.44
𝛽 = 7.53×105 cm-1
t = 65 𝜇s, start to melt v = 15 cm/s
t = 30 𝜇s, start to melt v = 0

## Slide 23: Present ALE3D Simulations
3D simulations for scanning laser
Scanning speed v = 15 cm/s
P = 22.5 W; FWHM = 50 𝜇m
q0 = 282 J/cm2
𝜏 = FWHM/v = 333 𝜇s
Absorptivity: 0.44
𝛽 = 7.53×105 cm-1
t = 200 𝜇s, v = 15 cm/s
width = 31 𝜇m, depth = 4.5 𝜇m
t = 200 𝜇s, v = 0
width = 39 𝜇m, depth = 5 𝜇m

## Slide 24: Present ALE3D Simulations
3D simulations for scanning laser
Scanning speed v = 30 cm/s
P = 45 W; FWHM = 60 𝜇m
q0 = 235 J/cm2
𝜏 = FWHM/v = 200 𝜇s
Absorptivity: 0.44
𝛽 = 7.53×105 cm-1
t = 18 𝜇s, start to melt v = 30 cm/s
t = 17 𝜇s, start to melt v = 0

## Slide 25: Present ALE3D Simulations
3D simulations for scanning laser
Scanning speed v = 30 cm/s
P = 45 W; FWHM = 60 𝜇m
q0 = 235 J/cm2
𝜏 = FWHM/v = 200 𝜇s
Absorptivity: 0.44
𝛽 = 7.53×105 cm-1
t = 130 𝜇s, v = 30 cm/s
width = 67 𝜇m, depth = 12 𝜇m
t = 130 𝜇s, v = 0
width = 72 𝜇m, depth = 13 𝜇m

## Slide 26: Present ALE3D Simulations
3D simulations for scanning laser
Scanning speed v = 38 cm/s
P = 92 W; FWHM = 54 𝜇m
q0 = 396 J/cm2
𝜏 = FWHM/v = 142 𝜇s
Absorptivity: 0.44
𝛽 = 7.53×105 cm-1
t = 4 𝜇s, start to melt

## Slide 27: Present ALE3D Simulations
3D simulations for scanning laser
Scanning speed v = 38 cm/s
P = 92 W; FWHM = 54 𝜇m
q0 = 396 J/cm2
𝜏 = FWHM/v = 142 𝜇s
Absorptivity: 0.44
𝛽 = 7.53×105 cm-1
t = 25 𝜇s, reaches the boiling point!

## Slide 28: Melting of Stainless Steel
P = 22.5 W, FWHM = 50 𝜇m
Absorptivity = 0.44
t = 200 𝜇s
P = 45 W, FWHM = 60 𝜇m
Absorptivity = 0.44
t = 130 𝜇s
P = 92 W, FWHM = 54 𝜇m
Absorptivity = 0.33
t = 25 𝜇s

## Slide 29: Conclusions and Future Work
We have simulated laser heating and melting bulk stainless steel.
In 2D simulations, we investigated the relations between melt hole size and model parameters, including optical properties of steel and powder distribution of laser, for zero scanning speed.
In 3D simulations, we studied melting processes using three laser beams with different power, size, and scanning speed.
In the future we’ll study
  electron beam heating and melting metals
  electron beam processing metallic powder materials